Information regarding the requirements of the Pressure Equipment Directive 2014/68/EU.

Dovre Sertifisering AS

GUIDELINE

GL-DSE-2020-006 Acceptance of using TR2000 and ASME under PED 2014/68/EU

NORMAL CARBON STEEL (CSNT), Not impact tested

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |
|  |  |  |  |  |  |
|  |  |  |  |  |  |
| 01 | 25.11.2020 | Changed number of document | RB | LS | All |
| 00 | 31.10.2019 | For approval | RB | SB | All |
| Rev | Date | Description | Prepared | Checked | Client |

|  |  |
| --- | --- |
| Document title: | Acceptance of using TR2000 and ASME under PED 2014/68/EU |
| Client: | All |
| Client order: | All |
| DSE number: | GL-DSE-2020-006 Material using TR2000 and ASME CSNT |

Contents

[1. Materials included in this document 2](#_Toc23417153)

[2. Properties for allowable stress 2](#_Toc23417154)

[3. Temperature and toughness 2](#_Toc23417155)

[4. Welding and NDT 3](#_Toc23417156)

[5. Ductility 3](#_Toc23417157)

[6. Forming 3](#_Toc23417158)

[7. Documentation and marking 3](#_Toc23417159)

[8. Abbreviations 4](#_Toc23417160)

# Materials included in this document

|  |  |  |
| --- | --- | --- |
| **Standard** | **Grade** | **Form** |
| ASTM A106 | B | Pipe |
| API 5L | PSL 1 E | Pipe |
| A672 | C60 | Pipe |
| A234 | WPB | Pipe fittings |
| A105 |  | Forging |
| A516 | 60 | Plate |
| A516 | 70 | Plate |

# Properties for allowable stress

Allowable stresses within the applicable temperature range are defined in ASME B31.3 for

each material grade (Table A-1).

# Temperature and toughness

These materials require ISO Charpy V impact testing if they are used at temperatures below 00C.

Since the MDS limits the chemical composition and the stresses are 20% lower than for the European Harmonised standards, these materials are not to be used below -150C.

For use of A105 down to -290C the following requirements are made.

* Material is Grain refined.
* Normalising heat treatment.
* Reduction ratio is at least 4:1.

# Welding and NDT

If materials are used for welding there are restrictions with respect to C, S, P and the defined CE found in EN13480

The weldability is sufficient.

Welding procedures and operators

Directive 2014/68/EU §3.1.2 requires that for equipment in Category II, III and IV the operating procedures and operators are qualified by a recognised third-party organisation within the European Community or a Notified Body. Dovre Sertifisering AS has Notified Body number 2654.

NDT personnel

Directive 2014/68/EU §3.1.3 requires that NDT personnel is qualified. For pressure equipment in categories III and IV, the personnel shall be approved by a third-party organisation recognised by a Member State pursuant to article 20.

# Ductility

The Directive 2014/68/EU §7.5 requires a steel sufficiently ductile. Elongation after rupture is no less than 14 % at a temperature not higher than the lowest scheduled operating temperature as mentioned under §3 of this document.

All the specified materials have minimum ductility exceeding 14% thus, fulfilling the Directive 2014/68/EU ductility requirements

# Forming

The bending radius shall not be less than 3 times the outer pipe diameter. This is required to reduce the risk for strain ageing.

# Documentation and marking

The inspection documentation in accordance with EN 10204:2004 is specified in the MDS.

All MDS’s require marking of the material ensuring full traceability to the melt.

The requirements in the Directive 2014/68/EU are found fulfilled.

# Abbreviations

C Carbon

S Sulphur

P Phosphorous

CE Carbon Equivalent

NDT Non-Destructive Testing